SAUDI ARAMCO

MATERIAL REQUISITION FOR INQUIRY

MRQ No.: MRQ-2024-VAL-0391   |   Rev. 0   |   Date: 15-Jan-2024

Gate Valves — Carbon Steel, Class 300, API 6D

# 1. Scope of Supply

The Vendor shall design, engineer, manufacture, inspect, test, and deliver Carbon Steel Gate Valves in strict accordance with the requirements set forth in this Material Requisition, applicable Saudi Aramco Engineering Standards (SAES), and the referenced industry codes listed herein.

The following quantities are required:

| Item | Description | Size | Qty | Delivery (Weeks) |
| --- | --- | --- | --- | --- |
| 1 | Gate Valve, CS, Class 300, RF, BW, API 6D | 4" | 12 | 16 |
| 2 | Gate Valve, CS, Class 300, RF, BW, API 6D | 6" | 8 | 16 |
| 3 | Gate Valve, CS, Class 300, RF, BW, API 6D | 8" | 6 | 18 |
| 4 | Gate Valve, CS, Class 300, RF, FLG, API 6D | 10" | 4 | 20 |
| 5 | Gate Valve, CS, Class 300, RF, FLG, API 6D | 12" | 2 | 20 |

# 2. Applicable Codes and Standards

All valves shall be designed and manufactured in accordance with the latest edition of the following codes and standards:

- API 6D — Specification for Pipeline and Piping Valves

- ASME B16.5 — Pipe Flanges and Flanged Fittings

- ASME B16.25 — Buttwelding Ends

- ASME B16.34 — Valves — Flanged, Threaded, and Welding End

- ASTM A216 WCB — Standard Specification for Steel Castings

- SAES-L-108 — Selection of Valves

- SAES-L-350 — Construction of Plant Piping

- NACE MR0175 / ISO 15156 — Sour Service Requirements

# 3. Technical Specifications

## 3.1 Design & Pressure-Temperature Ratings

Valves shall be full bore (full opening) design. Reduced bore valves are not acceptable under any circumstances.

Design pressure: 740 psi (51 bar) at design temperature of 250°F (121°C).

The shell test pressure shall be 1,110 psi and the seat test pressure shall be 740 psi, both conducted with water as the test medium per API 6D.

## 3.2 Materials of Construction

| Component | Material / Standard |
| --- | --- |
| Body & Bonnet | ASTM A216 Gr. WCB (Carbon Steel Casting) |
| Gate (Wedge) | ASTM A216 Gr. WCB with 13% Cr overlay on seating surfaces |
| Stem | ASTM A182 Gr. F6a (13Cr Stainless Steel) |
| Seat Rings | ASTM A182 Gr. F6a, hard-faced with Stellite 6 |
| Bolting (Body/Bonnet) | ASTM A193 Gr. B7 studs / ASTM A194 Gr. 2H nuts |
| Packing | Flexible Graphite (Fire Safe) |
| Gasket | Spiral Wound, 316SS/Flexible Graphite with CS outer ring |

## 3.3 End Connections

Butt weld (BW) ends per ASME B16.25 for sizes 4" through 8". Raised face flanged (RF FLG) ends per ASME B16.5 for sizes 10" and 12". All flange faces shall be serrated (125–250 AARH finish).

## 3.4 Operation

All valves shall be manually operated with rising stem and outside screw and yoke (OS&Y) configuration. Valve handwheels shall be sized for a maximum rim pull of 80 lbf to operate against full differential pressure.

Gear operator shall be provided for all valves 10" and above.

# 4. Quality and Inspection Requirements

## 4.1 Quality Management System

The Vendor shall hold a current ISO 9001:2015 certification. A copy of the certification shall be included with the bid. The Vendor's Quality Management System (QMS) shall be subject to audit by Saudi Aramco at any time during the contract period.

## 4.2 Inspection & Test Plan (ITP)

The Vendor shall submit a detailed Inspection & Test Plan (ITP) for Saudi Aramco review and approval within 14 days of purchase order award. Witness points (W) and Hold points (H) shall be defined for each activity.

Mandatory witness/hold points include:

- Chemical composition and mechanical properties review (H)

- Non-Destructive Examination (NDE) — 100% visual, 10% RT on welds (W)

- Shell hydrostatic test (H) — Saudi Aramco Inspector witness mandatory

- Seat leakage test (H)

- Final dimensional inspection (W)

- Factory Acceptance Test (FAT) — full function test (H)

# 5. Safety Requirements

All valves shall comply with Saudi Aramco General Instruction GI-0002.100 — Safety in Design.

Fire-safe design is mandatory. Valves shall be fire-tested and certified per API 607 or API 6FA. Fire-safe certification documents shall be included in the bid.

Valves in sour service shall comply with NACE MR0175 / ISO 15156 for all wetted metallic components. The Vendor shall declare H₂S service compliance explicitly in the bid submittal.

# 6. Documentation Requirements

The following documentation shall be submitted with the bid:

- Completed Bid Tabulation Sheet (BTS) per Saudi Aramco format

- Dimensional drawings (GA drawings) for each valve size

- Sectional assembly drawings showing all components

- Material certificates (EN 10204 Type 3.1) for pressure parts

- ISO 9001:2015 Quality Certificate

- API 607 / API 6FA Fire-Safe Test Certificate

- Deviations list (if any) — no deviations from SAES are acceptable without formal waiver

- Manufacturing record book (MRB) table of contents

# 7. Commercial Terms

## 7.1 Validity

Bid prices shall remain valid for a minimum of 90 days from the bid submission deadline.

## 7.2 Delivery

Ex-Works (EXW) delivery basis. Packing and preservation shall be per Saudi Aramco SAES-L-460. Vendor is responsible for all export documentation.

## 7.3 Warranty

The Vendor shall provide a minimum 24-month warranty from the date of delivery, covering all defects in material and workmanship.

## 7.4 Liquidated Damages

Liquidated damages (LD) for late delivery: 0.5% of the total purchase order value per week of delay, up to a maximum of 10% of the purchase order value.

# 8. Submission Instructions

Bids shall be submitted electronically via the Saudi Aramco Supplier Portal (portal.aramco.com) no later than 12:00 noon (AST) on 15-Feb-2024. Late bids will not be considered.

Technical and commercial submissions must be in separate sealed envelopes (or separate PDF attachments). Any commercial information included in the technical submission will result in disqualification.